## Slide 1: Elemental doping and phase transition of TiO2 induced by shock waves
Pengwan CHEN, Xiang GAO, Naifu CUI, Jianjun LIU*
Beijing Institute of Technology
*Beijing University of Chemical Technology

## Slide 4
Beijing Institute of Technology (BIT) was founded in 1940;
3,500 teachers and research staff;
51,000 students, including 8,200 master students , 2,500 Ph.D students;
5 campuses, 18 schools.

## Slide 5
BIT Main Campus
LiangXiang Campus
Zhuhai Campus
West Mountain Campus

## Slide 6: State Key Laboratory of Explosion Science and Technology (SKLEST)
Research areas:
Theory and Applied Technology of Energetic Materials;
Detonation and Explosion Technology;
Impact Dynamics of Materials;
Explosion Effects and Protection Technology;
Explosion Safety and Assessment.

## Slide 7: Facilities
Φ 57mm gas gun
Φ 37mm gas gun
two-stage gas gun
three-stage gas gun (under construction)

## Slide 8: Facilities
Electric gun
Shock wave tube

## Slide 9: Facilities
Explosion chamber and Flash x-ray
High speed camera
VISAR

## Slide 10
Explosion chamber

## Slide 11
Detonation-synthesized diamond
Shock-synthesized diamond

## Slide 12
Explosive welding

## Slide 13
Explosive hardening
Explosive powder compaction

## Slide 14: Explosive welding in China
More than 10 plants dealing with explosive cladding;
Output value of explosive clad metals is ¥6-7 billion ($1 billion) in 2011;
About 15 research institutes engaged in explosive production of new materials;
National conference on explosive synthesis of materials is held every year.

## Slide 15
International Explosives, Propellant and Pyrotechnic Symposium
International Safety Science and Technology Symposium
International Workshop on Intensive Loading and Its Effects
International conferences organized

## Slide 16
Academic exchange

## Slide 17: Outline
2
3
4
Shock induced doping of TiO2
Shock synthesis of high pressure phase of TiO2
Photoresponse properties of shock treated TiO2
1
Introduction

## Slide 18: Elemental doping of TiO2
TiO2 semiconductor has oxidative capacity, chemical stability and low cost advantages.
Main drawback: energy gap is rather large, thus TiO2 is only active in the ultraviolet region (λ<420 nm) accounting for less than 5% of the natural solar light.
Element-doped TiO2 will enhance visible-light absorption and reduce energy gap.
Conventional doping methods: Sputtering; Ion implantation; Chemical vapor deposition; Hydrolysis.

## Slide 19: Elemental doping of TiO2
TiO2(anatase)
Eg=3.2eV;
ex387nm
Et 3%

## Slide 20: Phase transition of TiO2
Three common phases of TiO2 in nature
Anatase (Eg=3.2 eV)
rutile (Eg=3.2 eV)
brookite (Eg=3.4 eV)
High-pressure phases (Srilankite, columbite, baddeleyite, fluorite) may exhibit different electronic and optical.
Srilankite TiO2 has been observed by shock induced phase transition, but pure phase has not been obtained.

## Slide 21: Materials
Precursors for doping:
P25 TiO2 (15-20 nm)
H2TiO3
Nitrogen doping resources :
dicyandiamide (DCD, C2N4H4)
hexamethylene tetramine (HMT, C6N4H12)
sodium amide (NaNH2)
ammonium nitrate(NH4NO3)
Precursor for high-pressure phase synthesis:
MC-150 TiO2 ( 5 nm)
T2 TiO2 ( 100 nm)

## Slide 22: Content
2
3
4
Shock induced doping of TiO2
Shock synthesis of high pressure phase of TiO2
Photoresponse properties of shock treated TiO2
1
Introduction

## Slide 23: Effects of shock wave intensity
sample
P25 TiO2 +10wt% C2N4H4
P25 TiO2 +10wt% C2N4H4
P25 TiO2
P25 TiO2 +10wt% C2N4H4
P25 TiO2 +10wt% C2N4H4
700
Flyer
Velocity
(km/s)
-
1.20
1.90
2.25
Shock
Pressure
(Gpa)
-
6.3
11.9
15.8
18.3
Shock
Temperature
(K)
Cutoff
wave
Length
(nm)
2000
1800
1300
400
N-doped
Concentr
ation(at%)
Band-gap
Width
(ev)
Anatase
Phase
Content
(%)
Rutile
Phase
Content
(%)
Srilankite
Phase
Content
(%)
-
2.52
435
698
710
730
3.10
2.85
1.78
1.75
1.70
-
3.67
9.22
11.28
13.45
50.7
67.7
81.9
85.3
46.9
14.7
18.1
21.0
27.5
30.1
23.0
21.8
11.3
0
0
P25 TiO2 +10wt% C2N4H4
3.37
29.4
2700
765
1.62
13.58
21.1
24.9
54.0

## Slide 24
XRD analysis
Srilankite content (%)
54
23
21.8
11.3
0
XRD patterns of shock-recovered samples at different conditions
Unshocked P25 TiO2 (a),
shock-recovered C serial sample(P25+C2N4H4(10%)) at 1.20km/s (b),
1.90km/s (c), 2.25km/s (d), 2.52km/s (e) and 3.37km/s (f)

## Slide 25
200
300
400
500
600
700
800
f
e
d
c
b
a
Absorbance
Wavelength/(nm)
Phase change
Nitrogen doping
Shock induced Activation
UV-vis Spectra of Recovered sample
P25 TiO2 raw material (a); shocked P25 TiO2 (b);
shock-recovered A, B, C serial samples at 2.25km/s (c, d, e)
A: P25+C2N4H4 (1%), B: P25+C2N4H4 (5%), C: P25+C2N4H4 (10%)

## Slide 26: Content
2
3
4
Shock induced doping of TiO2
Shock synthesis of high pressure phase of TiO2
Photoresponse properties of shock treated TiO2
1
Introduction

## Slide 27
Experimental conditions and results of shock induced phase transition

## Slide 28
XRD analysis
Unshocked MC-150 TiO2 (a), shocked MC-150 TiO2 at 2.56 km/s (b)
shocked MC-150(10%)+Cu at 2.73 km/s (c), 3.07 km/s (d)，3.37 km/s (c)

## Slide 29: Synthesis of high-pressure phase of TiO2（T2)
XRD patterns of shock-recovered samples shocked Cu+ T2(20 %),a-b,at 3.37km/s

## Slide 31
UV-vis Spectra of Srilankite TiO2
Raman Spectra of Srilankite TiO2

## Slide 32: Thermal stability
TG-DSC
XRD at elevated temperatures
300℃(a),400℃(b),500℃(c),600℃(d),700℃(e),800℃(f),900℃(g),1000℃(h),1100℃(i)

## Slide 33: Content
2
3
4
Shock induced doping of TiO2
Shock synthesis of high pressure phase of TiO2
Photoresponse properties of shock treated TiO2
1
Introduction

## Slide 34: Photocatalytic evaluation of N-doped TiO2 and high pressure phase TiO2
Schematic of photocatalytic degradation
Xenon lamp; 2. Rubber stopper; 3. Reactor; 4.Water and photocatalyst;
5. Stirrer; 6. dark box

## Slide 35
Photocatalytic degradation of rhodamine B using N-doped TiO2
(Moderate shock intensity is preferred)
P25 TiO2+10wt%C2N4H4 1.2 km/s(a), 2.52 km/s(b), 2.25 km/s(c), 1.90 km/s(d ),
1.79 km/s(h);(e) P25 TiO2+5wt%C2N4H4 2.25 km/s;
(f) P25 TiO2+1wt%C2N4H4 2.25 km/s; (g) P25 TiO2 2.25 km/s

## Slide 36
Photocatalytic degradation of
different samples to methylene blue (MB)
(a)P25+C2N4H4(10%) at 2.25km/s;
(b)H2TiO3+ C2N4H4(10%) at 2.74km/s;
(c)H2TiO3+ C2N4H4(10%) at 2.25km/s.
Photocatalytic degradation of
different samples to Rhodmine B (RB)
(a)P25+C2N4H4(10%) at 2.25km/s;
(b)H2TiO3+ C2N4H4(10%) at 2.25km/s;
(c)H2TiO3+ C2N4H4(10%) at 2.74km/s.

## Slide 37
Photocatalytic Degradation of Methylene blue using high-pressure phase TiO2
(a) MC-150TiO2+90wt%Cu 3.07 km/s; (b) MC-150 TiO2+90wt%Cu 3.37 km/s

## Slide 38: Photo electrochemical activity of TiO2 after shock processing
I-V
Powder sample and Graphene

## Slide 39: Photo electrochemical activity of N-doped TiO2
0.008 10-4A
5times
0.04 10-4A
10times
0.08 10-4A
Photo electrochemical activity of N-doped TiO2 under visible light irradiation
(a) Raw TiO2; (b) shock treatment at 1.2km/s; (c) shock treatment at 2.25km/s

## Slide 40: Photo electrochemical activity of high-pressure phase of TiO2
Good stability

## Slide 41: DSSC performance of shock induced N-doped TiO2
sample
a/b/c
Flyer
velocity
(km/s)
1.20
Cutoff
wave
length
(nm)
450
N-doped
concentr
ation(at%)
Band-gap
width
(ev)
Anatase
phase
content
(%)
Rutile
phase
content
(%)
Srilankite
phase
content
(%)
2.76
0.76
71.4
11.8
16.8
a
b
c
Sample
a
b
c
Sample preparation
Isc(mA/cm2)
Voc(mV)
ff(%)
n(%)
Smear two layer and sinter
Smear one layer and sinter
Smear one layer and sinter
Smear one layer and sinter
Smear two layer and sinter
5.00
3.20
0.71
753
725
738
7.30
1.66
2.66
4.17
0.75
0.76

## Slide 42: Conclusions
Nitrogen doped TiO2 was obtained by shock treatment of a mixture of TiO2 precursor and nitrogen resources. Nitrogen doped TiO2 exhibits enhanced visible-light photocatalytic activity.
Pure Srilankite TiO2 can be obtained by shock-induced phase transition;
Shock-induced doping might be a promising method for powder modification.

## Slide 43: Thank you for your attention! http://shock.bit.edu.cn E-mail: pwchen@bit.edu.cn