## Slide 1: FABRICATION OF corrosion-resistanT multilayer materials by explosive welding
PENZA STATE UNUVERSITY
PENZA , RUSSIA

## Slide 2: Anodic and cathodic polarization curves

## Slide 3: The corrosive influence on multilayer material

## Slide 4: The international application РСТ WO2010/036139 A1«Multilayer material with enhanced corrosion-resistance (variants) and methods for preparing same»
USA, Japan, Korea, China, Ukraine
European Patent Office
Eurasian Patent Organization

## Slide 5: Multilayer materials by explosive welding
stainless steel – carbon steel - stainless steel
12Х18Н10Т – 20 – 12Х18Н10Т
stainless steel – carbon steel - stainless steel - low-alloyed steel
12Х18Н10Т – 20 – 12Х18Н10Т – 09Г2С
stainless steel – copper - stainless steel
12Х18Н10Т – M1 – 12Х18Н10Т

## Slide 6: The requirements of certification
Testing of corrosion resistant
Testing of stress-strain properties
Testing of technological properties

## Slide 7: BASE STANDARTS
GOST 9.912 United system of corrosion and ageing protection. Corrosion resistant steels and alloys. Methods of accelerated tests for resistance to pitting corrosion
BS EN ISO 11463:2008 Corrosion of metals and alloys. Evaluation of pitting corrosion
ASTM G48 - 11 : Standard Test Methods for Pitting and Crevice Corrosion Resistance of Stainless Steels and Related Alloys by Use of Ferric Chloride Solution

## Slide 8: Pitting corrosion in stainless steel

## Slide 9: Calculation of pittings on protected surface

## Slide 10: Anode solution reactions of protector
Аnode | Cathode
Fe0 → Fe+2 + 2e | Fe+3+ 2e → Fe+2 2H+ + 2e → H2

## Slide 11: The quantitative measures
The number of holes on the unit of area
The depth of holes
The number of holes that was formed for long period

## Slide 12: Specimen with synthetic pittings

## Slide 13: The quantitative measures
The growth rate of the cavity in different environments
The hole diameter impact on growth rate

## Slide 14: Stainless steel – copper - stainless steel 12Х18Н10Т – M1 – 12Х18Н10Т

## Slide 15: The electrochemical test
The current test of short-circuited pair for different proportion between protector area and stainless steel area

## Slide 16: Skolkovo Innovation Centre
Project «Multilayer corrosion-resistant and heat-resistant material development, its technology and metal product fabrication»
André Rozen

## Slide 17: Skolkovo Innovation Centre
The benefits with regard to customs payments
The tax benefits
The access to the infrastructure of the Skolkovo Innovation Centre

## Slide 18: PENZA STATE UNIVERSITY
metal@pnzgu.ru
THANK YOU ATTENTION