## Slide 1: LAMINATED METAL–INTERMETALLIC COMPOSITES BY EXPLOSIVE WELDING AND ANNEALING
I. A. Bataev1, A. A. Bataev1, V. I. Mali2, M. A. Esikov2, P. S. Yartsev1, A.S. Gontarenko1
1. Novosibirsk State Technical Univestity
2. Lavrentyev Institute of Hydrodynamics SB RAS

## Slide 2: Outline
1. Motivation
2. Structure of Al-Ti composite produced by explosive welding
3. Peculiarities of Al3Ti layer formation during annealing
4. Some results of mechanical tests
5. Conclusion

## Slide 3: Motivation
High specific stiffness
High heat resistance
Low density
Good results in fatigue and impact tests
Combining the properties of both the hard and refractory intermetallics and the ductile matrix
“Dilution” of titanium with cheaper aluminum reduces the cost of material

## Slide 4: Vecchio KS. Synthetic multifunctional metallic–intermetallic laminate composites. JOM 2005;57:25–31.

## Slide 5: Scheme of explosive welding
Al plate – 1mm
Ti plate – 0,5 mm
HE – Ammonite 6GV

## Slide 6: Cross-section of explosively welded Al-Ti composite (optical microscopy)

## Slide 7: Interface appearance in the upper and lower parts of the composite
Upper part of composite
lower part of composite

## Slide 8: TEM investigation of the interface

## Slide 9: Vortexes arised during explosive welding
Al distribution
Ti distribution

## Slide 10: Vortexes structure (TEM)

## Slide 11: Dynamic of Al3Ti layer growth (630 oC annealing)
1 hour
5 hours
100 hours
Wavy interfaces
plane interfaces

## Slide 12: Al3Ti layer thickness at different interfaces after annealing at 630 oC
5 hours annealing
100 hours annealing

## Slide 13: 5 hours at 630 oC, layer thickness

## Slide 14: Growth of Al3Ti at the position of former vortexes
Growth of Al3Ti at plane interface
630 oC annealing, 30 min

## Slide 15: Scheme of Al3Ti layer growth

## Slide 16: Dependence of intermetallic layer thickness on annealing time

## Slide 17: XRD pattern after 100 hours at 630o

## Slide 18: TEM of intermetallic layer
Al3Ti

## Slide 19: Differences in Al3Ti grain size in different zones
Near Al
Middle of the Al3Ti layer
Near Ti
Al
Al3Ti
Ti

## Slide 20: Iron-reach intermetallic precipitations (100 hours 630 oC)
Dark field OM
Btight field OM
Btight field OM,
Iron-rich precipitation in the Al-layer

## Slide 21: Impact behavior of Al –Al3Ti – Ti composite
Al –Al3Ti – Ti
Al – Ti
Al3Ti
Ti

## Slide 22: Scheme of fatigue cracks propagation

## Slide 23: Fatigue fracture of Al3Ti layer

## Slide 24: Conclusion
Explosive welding of Ti and Al plates with subsequent annealing is effective technological process for MIL composites production.
Titanium trialuminide (Al3Ti) is the only intermetallic compound between Al and Ti formed under annealing.
The most favorable place for Al3Ti growth are former vortexes
The best intermetallic structure is on the Ti-Al3Ti boundary. On Al-Al3Ti boundary pores and microcracks were found
One of the most important goals arisen during explosive welding and annealing is addressing the causes of residual stresses, pores and microcracks formation